GROW YOUR OWN
(KOMBUCHA)MASK

The bacterial leather we will grow consists of cellulose
    which is a structural compound mainly found in plants SCOBY leather
    is super flexible, it can be treated like traditional leather and dried
   into sheet form, or can be moulded around a
    form during the drying process
        This
        material has the potential to be an alternative to animal
        sourced textiles and their harmful environmental
        impacts You can grow it with
        the following steps and spread it by dividing your
        SCOBY

• 200 ml apple cider vinegar (or the liquid from a previous SCOBY)
• 200g granulated sugar

• 2 Black or Green Tea Bags

• 2 Litre Water

Step 1: boil water
Step 2: let the tea infuse for about 15 minutes

    Step 3: dilute all the sugar (about 100 g per litre)

Step 4: let it boil for about 20-30 minutes with the lid on
 If you do not have a stove use the sugar tea water
        from the kit
        Step 5: let the liquid cool down to about 30°C

This is important:
higher temperatures risk killing the SCOBY when you add it. Leave
the lid on to keep nasties outside!
Make sure your liquid is below 30 °C. Make sure the container you
grow your leather in is cleaned well! And do these steps without
pausing, since you don’t want to expose your liquid to the air for too
long. This is to avoid infections
STARTING THE GROWTH
Step 6: pour the tea/sugar liquid into the container and add the
SCOBY and/or starter liquid
Step 7: cover the container with cloth Make sure the cloth doesn’t touch the liquid

  GROWTH

It’s good to know that your final sheet of leather will shrink
quite a bit: 10x to 15x times So if you have a specific thickness
of leather in mind, knowing when to stop growth will come from
experience

Step 11: remove the cloth and take out upper sheet of wet
scoby Rinse it and wash it with soap in the sink.
Pro-tip:
let your liquid grow again or save it to start
your next batch
Step 12: let your sheet dry on a wooden board It will take a
day or a few days depending on the temperature Don’t dry it at
too high a temperature, or the sheet will shrink in wrinkled way
To make sure your sheet does not stick to the board, turn it
around at least once per day This will also make the drying
process more homogenous
If you put it in the sun and depending on the thickness of the scoby it can take between 2 and 4 days of drying time
Step 13: when the sheet feels dry and doesn’t smell so much
like vinegar anymore, it’s done!!! Congratulations!